Table 1. Geometrical characteristics of the analysed models of stiffened plates.

| Type | Model | Shape | hw | tw | bf | tf | I [cm4] | q [kg/m]* | Zmin [cm3]* |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | F1 | flat | 177 | 14 | - | - | 647 | 101.1 | 149 |
| 1 | T1 | tee | 150 | 9 | 90 | 12 | 648 | 100.7 | 213 |
| 1 | A1 | angle | 150 | 9 | 90 | 12 | 648 | 100.7 | 213 |
| 2 | F2 | flat | 270 | 17 | - | - | 2,788 | 117.7 | 394 |
| 2 | T2 | tee | 250 | 10 | 90 | 15 | 2,844 | 111.9 | 526 |
| 2 | A2 | angle | 250 | 10 | 90 | 15 | 2,844 | 111.9 | 526 |
| 3 | F3 | flat | 445 | 16 | - | - | 11,749 | 137.5 | 947 |
| 3 | T3 | tee | 400 | 12 | 100 | 17 | 11,860 | 132.7 | 1,211 |
| 3 | A3 | angle | 400 | 12 | 100 | 17 | 11,860 | 132.7 | 1,211 |

* Zmin includes width 800 mm of the plate having thickness of 13 mm

Table 2. Coefficients of thin-horse mode initial deflection as a function of plate aspect ratio [19].

| a/a/b | A01/t | A02/t | A03/t | A04/t | A05/t | A06/t | A07/t | A08/t | A09/t | A010/t | A011/t |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.1158 | -0.0276 | 0.1377 | 0.0025 | -0.0123 | -0.0009 | -0.0043 | 0.0008 | 0.0039 | -0.0002 | -0.0011 |
|  | 1.1421 | -0.0457 | 0.2284 | 0.0065 | 0.0326 | -0.0022 | -0.0109 | 0.001 | -0.0049 | -0.0005 | 0.0027 |
|  | 1.1458 | -0.0616 | 0.3079 | 0.0229 | 0.1146 | -0.0065 | 0.0327 | 0.000 | 0.000 | -0.0015 | -0.0074 |
|  | 1.1439 | -0.0677 | 0.3385 | 0.0316 | 0.1579 | -0.0149 | 0.0743 | 0.0059 | 0.0293 | -0.0012 | 0.0062 |
|  | 1.1271 | -0.0697 | 0.3483 | 0.0375 | 0.1787 | -0.0199 | 0.0995 | 0.0107 | 0.0537 | -0.0051 | 0.0256 |

Table 3. Geometric and material properties of Tanaka & Endo tests.

| Structure No. | L (mm) | b (mm) | t (mm) | hw (mm) | tw (mm) | hwtw | A03 (mm) | σYp (MPa) | σYs (MPa) | E (GPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| # D0 |  | 1440 | 6.15 | 110.0 | 9.77 | 11.26 | 0.101 | 234.2 | 287.1 | 205.8 |
| D0A |  | 1440 | 5.65 | 110.0 | 10.15 | 10.84 | 0.250 | 249.9 | 196.0 | 205.8 |
| D1 |  | 1200 | 5.95 | 110.0 | 10.19 | 10.79 | 0.143 | 253.8 | 250.9 | 205.8 |
| D2 |  | 1560 | 5.95 | 110.0 | 10.19 | 10.79 | 0.288 | 253.8 | 250.9 | 205.8 |
| D3 | 1080 | 1440 | 5.95 | 103.5 | 11.84 | 8.74 | 0.312 | 253.8 | 326.3 | 205.8 |
| D4 |  | 1440 | 5.95 | 118.5 | 7.98 | 14.85 | 0.119 | 253.8 | 284.2 | 205.8 |
| D4A |  | 1440 | 5.65 | 118.5 | 8.08 | 14.67 | 0.379 | 249.9 | 274.4 | 205.8 |
| D10 |  | 1200 | 4.38 | 65.0 | 4.38 | 14.84 | 0.515 | 442.0 | 442.0 | 205.8 |
| D11 |  | 1200 | 4.38 | 90.0 | 4.38 | 20.55 | 0.503 | 442.0 | 442.0 | 205.8 |
| D12 |  | 1440 | 4.38 | 65.0 | 4.38 | 14.84 | 0.523 | 442.0 | 442.0 | 205.8 |

Table 4. Summary of results for some of Tanaka & Endo tests.

| Structure No. | Tanaka & Endo | Present |  |
| --- | --- | --- | --- |
|  | (σUlt)FEM(σUlt)EXPERIMENT | (σUlt)FEM(σUlt)EXPERIMENT | Collapse mode |
| # D0 | 0.977 | 1.014 |  |
| D0A | 1.028 | 1.065 |  |
| D1 | 0.869 | 0.911 |  |
| D2 | 0.936 | 0.944 |  |
| D3 | 0.860 | 0.853 |  |
| D4 | 0.792 | 0.866 |  |
| D4A | 0.866 | 0.960 |  |

Table 5. Deformation mode and spread of plasticity for the plate of dimensions 1600×800×14 mm (AR=2) with 5-20 years exposure (magnification factor for deformation mode: 10).

| Case | Ultimate strength level | Final step |
| --- | --- | --- |
| Uncorroded t = 14 mm |  |  |
| 5-year t = 13.17 mm |  |  |
| 10-year t = 11.73 mm |  |  |
| 15-year t = 9.94 mm |  |  |
| 20-year t = 8.18 mm |  |  |

Table 6. Deformation mode and spread of plasticity for the plate of dimensions 2400×800×14 mm (AR=3) with 5-20 years exposure (magnification factor for deformation mode: 10).

| Case | Ultimate strength level | Final step |
| --- | --- | --- |
| Uncorroded t = 14 mm |  |  |
| 5-year t = 13.3 mm |  |  |
| 10-year t = 11.75 mm |  |  |
| 15-year t = 10.04 mm |  |  |
| 20-year t = 8.23 mm |  |  |

Table 7. Deformation mode and spread of plasticity for the plate of dimensions 1600×800×18 mm (AR=2) with 5-20 years exposure (magnification factor for deformation mode: 10).

| Case | Ultimate strength level | Final step |
| --- | --- | --- |
| Uncorroded t = 18 mm |  |  |
| 5-year t = 17.47 mm |  |  |
| 10-year t = 15.50 mm |  |  |
| 15-year t = 13.79 mm |  |  |
| 20-year t = 12.43 mm |  |  |

Table 8. Deformation mode and spread of plasticity for the plate of dimensions 2400×800×18 mm (AR=3) with 5-20 years exposure (magnification factor for deformation mode: 10).

| Case | Ultimate strength level | Final step |
| --- | --- | --- |
| Uncorroded t = 18 mm |  |  |
| 5-year t = 17.47 mm |  |  |
| 10-year t = 15.50 mm |  |  |
| 15-year t = 13.79 mm |  |  |
| 20-year t = 12.43 mm |  |  |